## Slide 1
Jana Schaber
Graduiertenkolleg “AccelencE”, Leimen, 09.10.– 11.10.2023
R&D of Photocathodes used for ELBE SRF Gun II

## Slide 2
Outline
Introduction 1.1 SRF Guns 1.2 Requirements on Photocathodes
ELBE SRF Gun II
Photocathodes for SRF Gun II 3.1 Cs2Te 3.2 p-GaN:Cs 3.3 Mg studies
Summary & Outlook

## Slide 3: BNL SRF gun
HZDR SRF gun-II
in user operation
SRF guns for CW high brightness beam
PKU DC-SRF gun
DESY SRF gun
KEK SRF gun
HZB SRF gun
1. Introduction
WiFEL gun
LCLS-II HE gun
Notes: Unterschied in Cavity: oben 1.3 GHz unten nur 120 MHz RF field.

## Slide 4
high QE, low thermal emittance, fast response time
robust , long lifetime
low dark current
1. Introduction
General requirements for photocathode in injectors
Specially for SRF guns:
clean for SC cavities
properties at cryogenic temperature
thermal conductivity, thermal expansion
(SC cathode) transition temp., critical magnetic field
Multipacting issue: secondary electron yield
heat load: laser heating, RF power deposition
Requirements for photocathodes in SRF gun

## Slide 5
J.Teichert et al. Successful user operation of a superconducting radio-frequency photoelectron gun with Mg cathodes. PRAB 24, 033401 (2021)
Cathode Temp ~ 80K
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
Notes: At HZDR we operate SRF gun II 1.3GHz cavity for CW THz user beam, the bunch charge is 200pC.
In 2014 commissioning with Cu
2016,2017 three time failure with Cs2Te on Mo
Till 2019 succeeded in cleaning and operating Mg. 2019 - 2020 stable operation with Mg ~ 1760 h beam time, ~ 57 C charge

## Slide 6
Teichert, J. et al. Successful user operation of the superconducting radio-frequency photo electron gun with Mg cathodes at ELBE. Physical Review Accelerators and Beams 24(33401) (2021), 1–30
easy to use
little dark current
QE258nm~10-5 -10-4
Cu cathode: gun commissioning
Highlight:
2019 - 2020 stable operation for users
200-250 pC, 100 kHz, 1760 hrs, ~ 57 C
Mg cathode: stable operation
Since 2020 for user operation
Providing ~200 pC, 2.3 ps, 50-100 kHz
2-3 months lifetime with QE 0.5%-1%
High QE (10-1) after laser cleaning
Long lifetime
No multipacting problem
repeatable
Cs2Te cathode: most time used
? Possible QE drops due to transport, multipacting, CW RF and beam operation
2. Normal conducting photocathodes for SRF guns
2.2 Semiconductor photocathodes in SRF Guns

## Slide 7
Cs2Te for HZDR SRF gun
2. Normal conducting photocathodes for SRF guns
2.2 Semiconductor photocathodes in SRF Guns
Cs2Te deposited on Cu, not on Mo
preparation is quite complex
Deposition of Te (3 - 10 nm), then Cs till photocurrent reaches a maximum
Cs2Te used in SRF Gun II with 1% QE
Notes: At the same time, we have paid effort to solve the problem with overheating of Mo plug. In 2019, we changed to Cu as substrates. Copper is not friendly for Cs2Te coating, lower QE in our preperation, but it works well in the RF field. Since then we use Cs2Te on copper as routine cathodes. Nearly 3 months we will change to a new one. Multipacting is one issue, leading QE dropping but cathode can reach 1% typically. Here I show a cathode not the best, not the latest one, at moment workingin gun. QE dropped down during transport and RF turning on, and the distribution changed during operation, one border shows more robust. The thermal emittance is found strongly coupled to the QE distribution. Higher QE, higher thermal emittance. Film with difference Te thickness from 3nm – 10nm are prepared and installed in the gun, more details about QE evolution will be reported later together with surface chemical analysis.

## Slide 8
2. Normal conducting photocathodes for SRF guns
2.2 Cs2Te degradation under RF and QE inhomogenity
QE of 6 % after the preparation
Cs2Te is transportet into transport chamber
And it looses QE during transportation to the SRF Gun II
Shows 1-2 % QE in general in SRF Gun II
RF turning on, and the distribution changed during operation
The thermal emittance is found strongly coupled to the QE distribution.
Higher QE, higher thermal emittance.
Middle of photocathode lost QE more than border region

## Slide 9
2. Normal conducting photocathodes for SRF guns
2.2 Cs2Te degradation under RF and QE inhomogenity
Deposition of Te and Cs in the border region not fully overlapped
Border region and the middle are not consitent in Cs:Te ratio
 Contains less Cs than in the middle

## Slide 10
p-GaN(Cs) as potential new cathode
2. Normal conducting photocathodes for SRF guns
UHV preparation chamber (average 3 x 10-10 mbar)
310 nm UV-LED with 50 µW
Black body for thermal cleaning
Backside heating by manipulator
External IR sensor for temperature measurement
XPS chamber (average 5 x 10-9 mbar)
Schaber, J., Xiang, R. et al. Influence of surface carbon on the performance of cesiated p-GaN photocathodes with high quantum efficiency. Sci Rep 13, 3188 (2023).
Notes: GaN is interesting because it has high QE at third harmonic of laser and robust as Cs2Te
At HZDR we are studying this cathode with commercial p-GaN on sapphire / Si / SiC, activation only with cesium, QE~ 11.5 % and lifetime~ 5000 h in storage, and we study the degradation process with XPS, the first result shows when QE drops down, there is Ga2O3 appeared.

## Slide 11
Thermal cleaning with black body
use T between 400-500 °C to reduce O and C surface amounts
but low C and O concentrations remained on the p-GaN surface  impurities from crystal growths process ?
p-GaN(Cs) as potential new cathode
2. Normal conducting photocathodes for SRF guns

## Slide 12
Apply 3 – 4 A through Cs dispenser
Constant Cs flux in good E-9 mbar range
Photocurrent starts to increase after 20 min
Aperture in front of LED is used to reduce photocurrent (relief of vacuum)
Photocurrent runs into plateau
Open the aperture to receive the maximum photocurrent 1 µA = 7.7 % QE
time/ min
pressure/ mbar
p-GaN(Cs) as potential new cathode
2. Normal conducting photocathodes for SRF guns

## Slide 13
wet chemically cleaned (H2O2:H2SO4) & thermal cleaned via halogen lamp
activated with a thin layer of cesium
high QE values ( > 10%) & long lifetimes at suitable temperatures !
Surface morphology of used p-GaN photocathodes
> 600° C: surface is destroyed  low QE & lifetime
@ 500° C: GaN surface smooth  higher QE & lifetime
> 600° C
500° C
Schaber, J.; Xiang, R.; et al. Influence of Surface Cleaning on Quantum Efficiency, Lifetime and Surface Morphology of p-GaN:Cs Photocathodes. Micromachines 2022, 13, 849. https://doi.org/10.3390/mi13060849
p-GaN(Cs) as potential new cathode-spectral response
2. Normal conducting photocathodes for SRF guns

## Slide 14
QE decays in general exponentially
Peaks shift toward lower BE:
Charging effects ?
X-Ray influence ?
CsxCy intensity increased during decay  responsible for the natural lifetime
Schaber, J., Xiang, R. et al. Influence of surface carbon on the performance of cesiated p-GaN photocathodes with high quantum efficiency. Sci Rep 13, 3188 (2023).
p-GaN(Cs) as potential new cathode-degradation
2. Normal conducting photocathodes for SRF guns

## Slide 15
Remaining Cs is beneficial for QE
 Achieving higher QE after new Cs deposition
QE decays exponentially & longer lifetime
Same effects in the degradation process were observed as before
2. Thermal cleaning
3. Cs-activation
4. QE decay
p-GaN(Cs) as potential new cathode-degradation
2. Normal conducting photocathodes for SRF guns

## Slide 16
Under static conditions:
QE decays exponentially
With XPS:
XPS accelerates the QE decay
 thermalization and Cs melting
p-GaN(Cs) as potential new cathode-degradation
2. Normal conducting photocathodes for SRF guns

## Slide 17
p-GaN(Cs) as potential new cathode-spectral response
2. Normal conducting photocathodes for SRF guns
Using halogenlamp with broad wavelength spectrum plus monochromator
Cut-off wavelength is at 360 nm for p-GaN:Cs photocathodes
P-GaN:Cs reached max. 21 % at 290 nm

## Slide 18
Os
Ob
C=O
CO-R
C-C
MgCOx
Mg0
MgO-R
after 25.5 h
after 19.5 h
IPA
0
1
2
0.1 % QE @ 275 nm UV (102 µW)
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
Surface O is reduced while bulk O shows up
C cannot be fully removed but lowered in ist concentrations
MgCOx at the beginning transforms into MgO-R and MgO
IPA
200 °C, 19.5 h
220 °C, 25.5 h

## Slide 19
RMS roughness = 5.95 nm for 10 x 10 µm sample surface
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
Thermal cleaning is not able to remove all C and O
shows a smooth surface
ex-situ SEM and AFM measurements  might not be the „real“ surface as under vacuum

## Slide 20
0.35 % QE @ 275 nm UV (102 µW)
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
After sputtering
Before sputtering
Original surface showed a a lot of surface O (Os)
A lot of C from air environment and IPA
Mg showed a lot of MgCOx
After 300 s: (Os) peak decreased and O in bulk showed up (Ob)
Continued sputtering: O almost disappeared
Still MgO-R in spectrum and intensive Mg0
IPA
1.5 keV Ar+ (300 s)
1.5 keV Ar+ (300 s)
1.5 keV Ar+ (480 s)
Os
Ob
C=O
CO-R
C-C
MgCOx
Mg0
MgO-R
COx

## Slide 21
RMS roughness: 8.35 +- 2.1 nm
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
Sputtering causes a rough surface,
Spikes might be act as field emitter ?
 More studies are needed
ex-situ SEM and AFM measurements  might not be the „real“ surface as under vacuum

## Slide 22
citric acid
Ar+ 1.5 keV, 10 min
Ar+ 2.5 keV, 20 min
Ar+ 3.0 keV, 40 min
after 1.5 keV
Citric acid
after 2.5 keV
after 3.0 keV
QE = 0.134 %
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
Cleaning with a citric acid solution does not result in a homogenous surface
Different phases of citrate on the Mg plug
Sputtering takes a lot of time  thick citrate layer
Some QE received
 Cleaning with citric acid and sputtering does not result in the best surface conditions
Os
Ob
C=O
CO-R
C-C
MgCOx
Mg0
MgO-R
COx

## Slide 23
4. Summary and outlook
Both metal and semiconductor cathodes can be safe in SRF guns
P-GaN:Cs shows high potential to be a future electron source
21 % QE @ 260 nm; 11.5 % QE @ 310 nm UV-LED
commercially available p-GaN
only Cs required to form a photocathode
p-GaN quality, especially C, is the limiting factor
Mg photocathode research
surface behaviour can be followed by in-situ XPS
O at surface decreased while O in bulk appeared
cleaning with IPA works best
Ar+ works but roughens the surface
Cs2Te
5-6 % QE after preparation on Cu substrate
1-2 % QE in SRF Gun II
loss of QE under RF field and operation
2-3 months used in SRF Gun II
 Mo substrate ?
 higher quality of p-GaN ?
 Softer method (Hatomic)
 laser cleaning ?
Notes: NC photocathodes proved in gun
Waiting for results of SC photocathodes in gun
Important: technical know-how
heat load, thermal contact, suppressing multipacting,
particle free operation, vacuum during transport and operation, …
Theoretical understanding and full characterization:
QE & intrinsic emittance vs. temperature & RF & beam operation

## Slide 24
from the ELBE SRF Group:
A. Arnold, P. Zwartek, S. Ma, P. Murcek, R. Xiang, J. Teichert, A. Ryzhov, A. Hoffmann, R. Niemcyk, S. Gatzmaga
Thank you for your attention!
Thanks to all of our project partners !
Visit us @ EWPAA 2024 !

## Slide 25
Wet chemical cleaning using simple solvents or acidic solutions to minimize surface contaminations
Thermal cleaning using black body or thermo-coupler to heat the surface and create an atomically clean surface
Cs activation by the deposition of a thin Cs layer on the cleaned surface
Degradation QE decay examination in a certain period; reaching 1 %
Re-activation of the same sample starting again at step 2
Wet chemical cleaning using simple solvents or acidic solutions to minimize surface contaminations
Thermal cleaning using black body or thermo-coupler to heat the surface and create an atomically clean surface
Cs activation by the deposition of a thin Cs layer on the cleaned surface
Degradation QE decay examination in a certain period; reaching 1 %
Re-activation of the same sample starting again at step 2
Wet chemical cleaning using simple solvents or acidic solutions to minimize surface contaminations
Thermal cleaning using black body or thermo-coupler to heat the surface and create an atomically clean surface
Cs activation by the deposition of a thin Cs layer on the cleaned surface
Degradation QE decay examination in a certain period; reaching 1 %
Re-activation of the same sample starting again at step 2
Wet chemical cleaning using simple solvents or acidic solutions to minimize surface contaminations
Thermal cleaning using black body or thermo-coupler to heat the surface and create an atomically clean surface
Cs activation by the deposition of a thin Cs layer on the cleaned surface
Degradation QE decay examination in a certain period; reaching 1 %
Re-activation of the same sample starting again at step 2
Wet chemical cleaning using simple solvents or acidic solutions to minimize surface contaminations
Thermal cleaning using black body or thermo-coupler to heat the surface and create an atomically clean surface
Cs activation by the deposition of a thin Cs layer on the cleaned surface
Degradation QE decay examination in a certain period; reaching 1 %
Re-activation of the same sample starting again at step 2
Results
Thermal cleaning with black body
2. Thermal cleaning
3. Cs-activation
4. QE decay

## Slide 26
J. Schaber, R. Xiang, J. Teichert, A. Arnold, P. Murcek, P. Zwartek, A. Ryzhov, S. Ma, S. Gatzmaga, P. Michel, N. Gaponik. „Influence of Surface Cleaning on Quantum Efficiency, Lifetime and Surface Morphology of p-GaN:Cs Photocathodes”. Micromashines, 2022, 13, 849. DOI: 10.3390/mi13060849
R. Xiang and J. Schaber. „Review of Recent Progress on Advanced Photocathodes for Superconducting RF Guns”. Micromachines, 2022, 13, 1241. DOI: 10.3390/mi13081241
S. Ma, A. Arnold, P. Michel, P. Murcek, A. Ryzhov, J. Schaber, R. Steinbrück, P. Evtushenko, J. Teichert, W. Hillert, R. Xiang, J. Zhu. „The application of encoder-decoder neural networks in high accuracy and efficiency slit-scan emittance measurements”. Nuclear Inst. and Methods in Physics Research, A 1050, 2023, 168125. DOI: 10.1016/j.nima.2023.168125
J. Schaber, R. Xiang, N. Gaponik. „Review of photocathodes for electron beam sources in particle accelerators”. J. Mater. Chem. C, 2023,11, 3162-3179. DOI:10.1039/D2TC03729G
J. Schaber, R. Xiang, A. Arnold, A. Ryzhov, J. Teichert, P. Murcek, P. Zwartek, S. Ma, P. Michel. „Impact of various cleaning procedures on p-GaN surfaces”. Surf Interface Anal. 2023;1–8. DOI: 10.1002/sia.7207
J. Schaber, R. Xiang, J. Teichert, A. Arnold, P. Murcek, P. Zwartek, A. Ryzhov, S. Ma, S. Gatzmaga, P. Michel. „Influence of surface carbon on the performance of cesiated p-GaN photocathodes with high quantum efficiency”. Scientific Reports, 2023, 13:3188. DOI: 10.1038/s41598-023-30329-0
Publications

## Slide 27
Cathode | Typical wavelength (nm) | QE @ room Temp. | EG+EA (eV) | Expected thermal emittance (µm/mm)
Cs2Te | 266 | 0.1 | 3.5 | 0.9
Cs3Sb | 432 | 0.15 | 1.6+0.45 | 0.7
K3Sb | 400 | 0.07 | 1.1+1.6 | 0.5
Na3Sb | 330 | 0.02 | 1.1+2.44 | 0.4
Na2KSb | 330 | 0.1 | 1+1 | 1.1
K2CsSb | 532 | 0.1 | 1+1.1 | 0.4
GaAs(Cs,O) | 532 | 0.1 | 1.4 | 0.44
GaN(Cs) | 250-360 | 0.2-0.3 | 3.4 -? | -
Cathode | Typical wavelength (nm) | QE @ room Temp. | EG+EA (eV) | Expected thermal emittance (µm/mm)
Cs2Te | 266 | 0.1 | 3.5 | 0.9
Cs3Sb | 432 | 0.15 | 1.6+0.45 | 0.7
K3Sb | 400 | 0.07 | 1.1+1.6 | 0.5
Na3Sb | 330 | 0.02 | 1.1+2.44 | 0.4
Na2KSb | 330 | 0.1 | 1+1 | 1.1
K2CsSb | 532 | 0.1 | 1+1.1 | 0.4
GaAs(Cs,O) | 532 | 0.1 |  | 0.44
GaN(Cs) | 250-360 | 0.2-0.3 | 3.4 -? | -
D.H. Dowell et al., NIMA 622, Pages 685-697 (2010)
Xiaohui Wang et al., J. Mater. Chem. C, 2021, 9, 13013
2. Normal conducting photocathodes for SRF guns
2.2 Semiconductor photocathodes in SRF Guns
Notes: I borrow a semiconductor overview table from Dr. Dowell, here one can see the cathodesfrom UV to green.

## Slide 28
1. Introduction
SRF gun - promising source for high brightness and high current beams required by CW FELs and ERL facilities.
high gradients on the cathode surface than DC guns – increasing achievable surface current density and reducing thermal emittance contribution;
high beam energy to mitigate space-charge effects on the way from the gun to the next accelerator cavity;
outstanding vacuum environment for sensitive cathodes;
low RF jitter for excellent e- beam and light source stability.
Notes: SRF guns have advantages for operating in continuous wave (CW) mode and generating the high-brightness and high-current beams required by CW X-ray free electron laser (XFEL) [1] [2] and energy recovery linac (ERL) facilities [3] [4]. Similar to the normal conducting rf guns, SRF guns are able to provide higher gradients on the cathode surface than DC guns, increasing the achievable surface current density and reducing the thermal emittance contribution for a given bunch charge; higher beam voltages help to mitigate space-charge effects as the beam travels from the gun to the next accelerator cavity. Concurrently, SRF guns have an outstanding vacuum environment for sensitive cathodes and potentially lower RF jitter compared to CW normal-conducting (NC) photoinjectors [5].

## Slide 29
Advantage: robust and „clean“ for SRF guns
Lide, D. R.. Properties of Solids, CRC Handbook of Chemistry and Physic, Internet Version 2005, P. 124;
S. Halas, Materials Science-Poland, Vol. 24, No. 4, 2006
D.H. Dowell et al., NIMA 622, Pages 685-697 (2010)
2. Normal conducting photocathodes for SRF guns
2.1 Metal photocathodes in SRF Guns
Metal | QE | ɸ (eV) | Tc (K)
Cu | 10-5 - 10-4 | 4.6 | 
Mg | 10-5 - 10-3 | 3.6 | 
Nb | 10-6 – 10-4 | 4.3 | 9.3
Pb | 10-6 - 10-3 | 4.2 | 7.2
Notes: Metals are Robust, easy for treatment and transport, good rf property, little risk for cavity contamination
always good choice for commissioning
In the list several metals mentioned in following slides, here we can see mg has lower work function than the others and possible to get high QE with 260nm UV laser.