## Slide 1: Benchmark calculation of the PHITS code for neutron attenuation in iron and concrete on shielding experiments at proton accelerator facilities
Norihiro Matsuda1, Yosuke Iwamoto1, Tatsuhiko Sato1, Shintaro Hashimoto1, Tatsuhiko Ogawa1, Takuya Furuta1, Shinichiro Abe1, Takeshi Kai1,
Ryuji Hosoyamada2, Hiroshi Iwase3, Hiroshi Nakashima1, and Koji Niita2
1 JAEA, Japan Atomic Energy Agency
2 RIST, Research Organization for Information Science and Technology
3 KEK, High Energy Accelerator Research Organization
SATIF-13, Helmholtz-Zentrum Dresden-Rossendorf
( Dresden, Germany, 10-12 October, 2016 )

## Slide 2: Introduction -1
For shielding designs and safety analyses of the J-PARC (Japan Proton Accelerator Research Complex), accuracy of PHITS (Particle and Heavy Ion Transport code System) were validated through benchmark calculations based on shielding experiments about 10 years ago.
The PHITS has been upgraded especially in the past five years.
Therefore, another round of benchmark calculations are required for the latest version of the PHITS.

## Slide 3: Introduction -2
Dr. HIRAYAMA has studied neutron attenuation through the inter-comparison in SATIF. Neutron attenuation length is very important for shielding calculations involving high-energy accelerators.
CONCRETE
H. Hirayama, Inter-comparison of medium-energy neutron attenuation in iron and concrete (8), SATIF-10
However, comparable experimental data is not exist.

## Slide 4: PURPOSE
In this study, benchmark calculations for shielding experiments at several proton accelerator facilities (TIARA, RCNP, AGS) are carried out with the latest version of the PHITS (ver. 2.82).
Moreover, we try to evaluate neutron attenuation length for these shielding experiments with the help of the PHITS.
TIARA: Takasaki Ion Accelerators for Advanced Radiation Application, JAEA
RCNP: Research Center for Nuclear Physics, Osaka Univ.
AGS: Alternating Gradient Synchrotron, BNL

## Slide 5: Models (default) in PHITS 2.82
INCL4.6 was introduced into PHITS version 2.52 (Dec., 2012) as substitute for Bertini model.

## Slide 6: Difference of neutron attenuations
For concrete, differences of neutron attenuations are observed for energies from 1 to 3 GeV.
H. Hirayama, Inter-comparison of medium-energy neutron attenuation in iron and concrete (8), SATIF-10
Max.(@ 3 GeV): ~10 g cm−2
← Bertini
PHITS ver. 2.82

## Slide 7: Tiara experiment
Experimental geometry & the source spectrum
68-MeV protons
99% enriched 7Li
Ex.) Concrete shield
100-cm thick 150-cm thick 200-cm thick
Peak region: 60-70 MeV
5.0×108
1.0×109
1.5×109
2.0×109
Quasi-mono energetic collimated neutrons are a produced this experimental facility.
～10 times

## Slide 8: Calculation results (TIARA)
TIARA (IRON)
TIARA (CONCRETE)
Overestimations are observed in the results at 100-cm-thick iron, and at 100- and 150-cm-thick concrete.
Expt.
Calc.

## Slide 9: Calculation results with JENDL-4.0/HE
TIARA (IRON)
TIARA (CONCRETE)
Overestimation was improved by using extended version of JENDL-4.0 (neutrons up to 200 MeV), JENDL-4.0/HE.
Expt.
Calc.
C. Konno, JENDL-4.0/HE benchmark test with concrete and iron shielding experiments at JAEA/TIARA, ICRS-13
(JENDL-4.0/HE)

## Slide 10: RCNP experiment
Experimental geometry & the source spectrum
140-MeV protons
enriched 7Li
Ex.) Concrete shield
100-cm thick 150-cm thick 200-cm thick
1.0×108
2.0×109
3.0×109
4.0×109
Peak region: 130-140 MeV
～10 times
Quasi-mono energetic collimated neutrons are a produced this experimental facility.
Geometry of RCNP is about the same as that of TIARA.

## Slide 11: Calculation results (RCNP)
RCNP (IRON)
RCNP (CONCRETE)
Expt.
Calc.
Calculated results both in iron and concrete are in good agreement with the experimental data on the whole.

## Slide 12: Attenuations of DOSE (TIARA & RCNP)
We try to evaluate neutron attenuation length based on the measured data at TIARA & RCNP.
(Dose equivalent rate is calculated from neutron spectrum with flux-to-dose conversion coefficient in inter-comparison.)
RCNP experiment (IRON)
Ex.)
100 g cm−2
Expt.
Calc.

## Slide 13: Attenuation length (TIARA & RCNP)
Neutron attenuation length are summarized for the shielding experiments at TIARA and RCNP.
If we want to put the obtained values of attenuation length on the figure, we must determine the incident neutron energy (horizontal axis in the figure) for the experiments.
<= for TIARA, 60-70 MeV (peak energy ???)
for RCNP, 130-140 MeV (peak energy ???)
Att. Length (g cm−2) | TIARA | RCNP
IRON | 73 (70- to 130-cm) | 100 (70- to 100-cm)
CONCRETE | 61 (150- to 200-cm) | 70 (150- to 200-cm)

## Slide 14: Peak and continuum spectrum
Continuum spectrum is unnecessary components to determine the incident energy in the experiment.
Hence, we analyzed contributions for dose equivalent rate from the peak and continuum spectrum separately.
peak
continuum

## Slide 15: Calculation results (TIARA)
5.0×108
1.0×109
1.5×109
2.0×109
continuum
TIARA (IRON)
Expt.
Calc.
Calc.
(continuum)
The continuum spectrum decreases with the thickness (depth).
However, the contribution for the dose equivalent rate from the continuum spectrum still remain about 7% at 100-cm thick.
RCNP expt.: 63~77%

## Slide 16: AGS experiment
Experimental geometry & neutron spectrum
2.83-GeV protons
Concrete
Iron
Iron
Mercury target
Activation detectors were installed in iron and concrete shield.
calculated by PHITS
lateral
spallation neutrons

## Slide 17: Calculation results (AGS)
AGS (IRON)
AGS (CONCRETE)
The calculated results are in good agreement with the experimental data.
88 g cm−2
93 g cm−2
149 g cm−2
149 g cm−2
We evaluated the neutron attenuation length from these data.
Expt.
Calc.

## Slide 18: Attenuation LENGTH (AGS)
Neutron attenuation length is summarized for AGS experiment.
Att. Length (g cm−2) | 209Bi(n, 4n)206Bi | 209Bi(n, 6n)204Bi
IRON | 149 (111- to 199-cm) | 149 (111- to 199-cm)
CONCRETE | 88 (229- to 320-cm) | 93 (229- to 320-cm)
Total
100-300 MeV
300-500 MeV
20-100 MeV
500-1,000 MeV
We divide the spallation spectrum into some energy region.
The Total dose attenuations from 100 to 200 cm depth depend on the attenuations by 100-300 MeV neutrons.
AGS (IRON)

## Slide 19: Attenuations of DOSE (AGS)
Total
100-300 MeV
300-500 MeV
20-100 MeV
500-1,000 MeV
AGS (IRON)
Neutron attenuations (slope) in AGS experiments are gradually changed with the depth by the flux and energy of the spallation spectrum.
We may obtain some attenuation length at different depth.

## Slide 20: Attenuation length
Attenuation length based on the measurements are summarized.

## Slide 21: Conclusion
In order to validate the accuracy of the latest version of PHITS (ver. 2.82), benchmark calculations were carried out for the shielding experiments at TIARA, RCNP, and AGS.
The calculated results by the PHITS (INCL4.6) were in good agreement with the measured ones on the whole, except for TIARA experiments.
Neutron attenuation length was summarized for each shielding experiment.
It is possible to obtain neutron attenuation length experimentally. However, we need more and more shield.

## Slide 22
Thank you for your attention.
E-mail: matsuda.norihiro@jaea.go.jp

## Slide 23: Attenuation length (CONCRETE)
Attenuation length (g/cm−2)
Source neutron energy (MeV)
TIARA
RCNP
AGS
PHITS ver. 2.82

## Slide 24: Models recommended to use in PHITS 2.24

## Slide 25: Difference of neutron attenuations
Neutron attenuations for iron make a slight change from 1 to 3 GeV.
H. Hirayama, Inter-comparison of medium-energy neutron attenuation in iron and concrete (8), SATIF-10
← Bertini
PHITS ver. 2.82

## Slide 26: Attenuation length (iron)
Attenuation length (g/cm−2)
Source neutron energy (MeV)
PHITS ver. 2.82
TIARA
RCNP
AGS

## Slide 27: Background
A Japanese Evaluated Nuclear Data Library (JENDL) special purpose file, JENDL-4.0 High Energy File (JENDL-4.0/HE), is an extended version of JENDL-4.0 for incident neutrons up to 200 MeV for 130 nuclei, and a nuclear data library for incident protons up to 200 MeV for 133 nuclei, which are relevant to high-energy applications. It was released in November, 2015.
More than 20 years ago shielding experiments at the Takasaki Ion Accelerators for Advanced Radiation Application (TIARA) in Japan Atomic Energy Agency (JAEA) were carried out for concrete and iron with quasi-mono energetic 40 or 65 MeV neutrons.

## Slide 28: Differences from the experiments
Calculation conditions of the inter-comparison are different from those of the shielding experiments.
 | Inter-comparison | TIARA expt. | RCNP expt. | AGS expt.
Neutron source | Mono-energy | Quasi-mono energy | Quasi-mono energy | Spallation spectrum
Shielding | Iron, Concrete | Iron, Concrete | Iron, Concrete* | Iron, Concrete
Thickness (cm) | Iron: 0-600 Conc.: 0-1200 | Iron: 0-130 Conc.: 0-200 | Iron: 0-100 Conc. : 0-200 | Iron: 0-330 Conc.: 0-500
Detector type (Geometry) | Surface cross (infinite) | Counter (finite) | Counter (finite) | Activation (≃infinite)
*: Low-activationized concrete (Ca-rich)
At least two data is needed to evaluate neutron attenuation length for the shielding experiments. For the measurements, we need to determine the energy of attenuation length.

## Slide 29: Calculation results (TIARA)
TIARA (IRON)
Expt.
Calc.
Calc.
(peak)
5.0×108
1.0×109
1.5×109
2.0×109
peak
The peak spectrum decreases with the thickness (depth).
And, the peak spectrum also make continuum spectrum.

## Slide 30: Calculation results (TIARA & RCNP)
For iron shield (20-, 40-, and 100-cm-thick)
TIARA expt.
RCNP expt.
Calculated results (100-cm-thick) were approximately made by the peak spectrum.
Expt.
Calc.
Calc.
(peak)

## Slide 31: Calculation results (TIARA)
Expt.
Calc.
Calc.
(peak)
TIARA (IRON)
5.0×108
1.0×109
1.5×109
2.0×109
5.0×108
1.0×109
1.5×109
2.0×109
peak
continuum
10～35%@ 100 cm
(Dose: ~7%)
Results around 100-cm depth is reliable.

## Slide 32: Attenuation of DOSE (TIARA & RCNP)
Attenuation of DOSE in iron and concrete was calculated with the models of the inter-comparison.
TIARA expt.
RCNP expt.
Total
Peak
Continuum
Depth in iron (cm)
Dose equivalent rate
(Sv per n/cm2)
Depth in iron (cm)
Dose equivalent rate
(Sv per n/cm2)
Peak (slow)
Continuum
(fast)
Peak (slow)
Continuum
(fast)
In a finite geometry (thickness), attenuation length using the neutron source in the experiments (Total) don’t reach the maximum one (peak energy).

## Slide 33: Neutron spectrum (AGS)
100-300 MeV
300-500 MeV
20-100 MeV
500-1,000 MeV

## Slide 34: Attenuation of DOSE (AGS)
Neutron attenuation length is summarized for AGS experiment.
Att. Length (g cm−2) | 209Bi(n, 4n)206Bi | 209Bi(n, 6n)204Bi
IRON | 149 (111- to 199-cm) | 149 (111- to 199-cm)
CONCRETE | 88 (229- to 320-cm) | 93 (229- to 320-cm)
Total
100-300 MeV
300-500 MeV
20-100 MeV
500-1,000 MeV
The dose attenuation from 100 to 200 cm depth depends on the decreasing by 100-300 MeV neutrons.
⇒ Any attenuations up to 1,000 MeV may be obtained by the depth.
AGS (IRON)

## Slide 35: Material composition
CONCRETE
Nuclide | TIARA (wt%) | RCNP (wt%) | AGS (wt%) | Inter-comparison (wt%)
H | 1.1 | 1.1 | 0.9 | 1.0
C | --- | 7.5 | 1.3 | 0.1
O | 48.2 | 49.6 | 48.3 | 53.9
Na | 2.0 | 0.3 | --- | ---
Mg | 1.1 | 0.6 | --- | 0.2
Al | 6.1 | 1.5 | 3.3 | 3.4
Si | 23.2 | 9.1 | 26.3 | 34.2
K | 1.1 | 0.1 | --- | 1.3
Ca | 12.4 | 32.5 | 14.2 | 4.4
Cr | --- | --- | 0.3 | ---
Fe | 6.0 | 0.8 | 2.0 | 1.4
← Lime stone
← Silica stone

## Slide 38: 台車＆検出器